Absorbacide Mineral Analysis

Organics Made Easy Absorbacide contains these minerals:

Silicon Dioxide (SiO2)	  	90.10%

Phosphorus Pentoxide (P2O5) 	0.03%

Aluminium Oxide (Al2O3)	4.62%

Titanium Dioxide (TiO2) 		0.37%

Iron Oxide (Fe2O3)		 3.16%

Vanadium Oxide (V2O5)		 0.03%

Manganese Oxide (MnO)	 0.02%

Chromium Oxide (Cr2O3)	 0.005%

Magnesium Oxide (MgO )	0.56%

Copper Oxide (CuO)		 0.004%

Calcium Oxide (CaO)		 0.62%

Zinc Oxide (ZnO)		 0.007%

Sodium Oxide (Na2O)		 0.11%

Potassium Oxide (K2O)		 0.06%

Sulphur Trixode (SO3)		 0.06%

Chlorine (Cl)			 0.05%