**Introduction to Nichigo G-Tape™**

Nichigo G-Tape is an innovative family of acrylic tapes manufactured by Nippon Gohsei, USA. Nichigo G-Tapes provide superior performance in construction and industrial applications while also being versatile enough to use for household tasks. All Nichigo G-Tape series share user friendly features and benefits; however, the series can be separated into two major categories: 1. Hard surface protection featuring residue free removal and 2. Permanent adhesion featuring exceptional performance in both high and low temperature extremes.

**Features and Benefits**

-Straight and clean tear by hand (All series)…No cutting tools needed.

-Excellent Water and Weather resistance (All series)

-Residue Free removal (Masking and Protection)

-Repositionable (All series)

-Stable performance in extreme low and high temperatures

-Meets AAMA 7-11 13 Type A Class 3 without primer (3040xx series)

- Removes from face to face adhesive contact cleanly with no loss of performance (All series)

**Representative Values**

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | **Marine** | **Masking and Protection** | | **HVAC** | **Permanent Adhesion Construction and Flashing** | | | **Double Sided** |
| **Properties** | **1008SW** | **1009xx** | **2010xx** | **2010AL** | **2020xx** | **3030xx** | **3040xx** | **9030xx** |
| **Roll Size(s)\*** | 2”x 82’ 2”x 164’ | 1”x 82’ 2”x 164’ | 2”x 164’ | 2”x 82’ | 2”x 164’  3”x 164’ | 2”x 65’ | 2”,4”,6”,9”,  12” x 65’ | 1”x 65’  2”x 65’ |
| **Thickness**  **(mil)** | 6.7 | 6.3 | 6.3 | 6.7 | 6.7 | 6.7 | 8.7 | 8.7 |
| **Adhesion Strength**  **Oz/in** | 36 | 40 | 44 | 44 | 90 | 105 | 140 | 133/133 |
| **Tensile Strength**  **Lbs/in** | 40 | 32 | 34 | 38 | 34 | 46 | 46 | 46 |
| **UV Exposure (months)** | 6-8 | 2-3 | 2 | 6-8 | 3-4 | 6-12 | 6-12 | N/A |

\*Check for availability in your local market