## Slide 1
‘Its all about the Science’
N Corduff FRACS
Director of Professional Education
Establishment Labs

## Slide 2: Breast Implant Choices and Trends in Australia
Anatomical or round
Smooth or textured
Upper pole fullness
cost
Bottoming out
ptosis
Double capsule
seromas
capsule

## Slide 3: Smooth Round Implants

## Slide 4
The Holy Grail of Biotech:
Biocompatability

## Slide 6
Breast Implants Surfaces
Dalby et al: fibroblasts filopodia sense
protrusions down to 10nm (0.01microns)
Notes: In this module we will review the behaviour of breast implant surfaces at a cellular level.

## Slide 7
                downregulated IL8, TNFa, TGFb1
                Upregulated collagen type 1 and vinculin
                Reduced inflammatory cytokine production
Breast fibroblasts:

## Slide 9
Motiva Implants® SmoothSilk®/SilkSurface®
SmoothSilk®/SilkSurface® 3D topography view taken with uSurf Mobile Profilometer per ISO 25178-2:2012
SmoothSilk®/SilkSurface® SEM image at a scale of 1 mm and 55X magnification
Notes: At the cellular level there is a fine surface topography which influences how cells behave

## Slide 10
Static friction: is the force that must be overcome to start moving the object.
Dynamic friction: relates to the force needed to keep a surface in motion at a constant velocity.
Tribology: Friction and Wear
Chart: Friction Coefficient
| Traditional Smooth | SmoothSilk®/SilkSurface® | "PU foam imprint" | "Salt-loss" texture
Static Friction Coefficient | 0.036 | 0.05 | 0.058 | 0.477
Dynamic Friction Coefficient | 0.025 | 0.03 | 0.014 | 0.088
Comparative of static and dynamic average coefficients of different breast implants available in the market. Testing Performed on Akron Rubber Development Laboratory, Inc. Results Property of Establishment Labs (2017).
Notes: The “salt-loss” texturing has a very high friction coefficient compared to surfaces with less roughness value.

## Slide 11
Roughness Comparison: ISO classification
Roughness values comparison between Smooth, SilkSurface® and macro-textures, measured with uSurf Mobile non-contact profilometer over 2.56 mm2. Results Property of Establishment Labs (2017).
Notes: There needs to be sufficient roughness at a cellular size to influence cell behaviour, but not enough roughness to cause friction with the tissues. In this graph the roughness of the SmoothSilk/SilkSurface® is almost that of a traditional smooth surface. It behaves like a smooth implant in the way it moves in the body but is very different in the way cells respond to its surface. It is this influence of the cellular behaviour that prevents unwanted encapsulation and fibrosis. It can be likened to etching on glass.

## Slide 12
Notes: The police are the first guys there, evqacuating and calling in the firefighters

## Slide 13
Implant Surface
Thrombus formation,
activated platelets fibrin
Notes: Blood and proteins associated with the injury stick to the implant surface. These proteins include complement, albumin, fibrinogen among others, and form a matrix for inflammatory cells.

## Slide 14
Notes: The local guys CFA fight the fire initially. They call in other local voluntary firefighters from home and work. After a few days they need to be replaced with more firefighters

## Slide 15
Implant Surface
Notes: Neutrophils are seen early in the acute inflammatory response. These are a type of blood white cell that sniff out and go to sites of injury. They are the cells that normally attack bacteria but try and destroy the implant by release of enzymes. The neutrophils realise they are ineffective after a few days and leave the job to the macrophages (career firefighters)

## Slide 16
Notes: With the realisation the fire is big interstate firefighting crews are called in

## Slide 17
Inflammatory macrophage
Monocytes
TNFa
IL 6
IL 1b
IL 8
Implant Surface
Notes: These (interstate firies) are like the monocytes. At the same time as neutrophils are heading in, other white blood cells, monocytes, are attracted into the area of injury and change into inflammatory macrophages. These inflammatory macrophages are angry and act like pacmen and normally engulph any foreign body substances, microbes, or cellular debris. They also try and bombard the implant surface with enzymes to try and destroy it. At the same time they send out lots of angry interleukin messages and cytokines to call in help from other cells such as mast cells involved in defence of the body.

## Slide 18
Notes: Specialised help being called in by satelite phone (interleukins) are water bombers “Elvis” (mast cells) The fire crews get organised into groups

## Slide 19
Inflammatory
macrophage
Frustrated
Inflammatory macrophage
Foreign Body Giant Cell
IL 4
IL 13
Mast cell
T helper cell
Implant Surface
Notes: These angry inflammatory macrophages get frustrated in not being able to destroy the implant and some of them group together and join forces, literally, into a foreign body giant cell to be more effective. This process is aided by attracted T helper cells (fire captains) and mast cells. Even these giant cells fail in breaking up and destroying the intruder implant.

## Slide 20
Notes: Once the fire is huge firefighters take another tack of containment and building firebreaks and bring in equipment to do so. We see the same in trying to wall of the large foreign body, breast implant

## Slide 21
Wound healing macrophage
Frustrated inflammatory macrophage
Inflammatory macrophage
Implant Surface
IL 10
Reduction of inflammation
PDGF
VEGF
TGFb
Fibroblast recruitment
Fibroblast activation and collagen deposition to form fibrous capsule
Notes: So, some of the macrophages are allocated to take a completely different approach. They convert into wound healing type macrophages. Their job is to concentrate not on destroying the implant but to reduce the inflammation and with the foreign body giant cells to organise its containment within a fibrous wall. The healing macrophages send out an IL10 message to slow down the angry response of its inflammatory macrophage colleagues. They along with the other inflammatory cells call in fibroblasts to deposit collagen to build the containing wall around the implant, the capsule. The normal inflammatory response would resolve once the wound is healed but because of the implant not being successfully “destroyed”, the healing macrophages, fibroblasts and other immune cells develop a long term plan of containment.

## Slide 22
Notes: Once the main fire has passed through engineers and managers start the building process and look to stronger containment lines for the future

## Slide 23
Lymph Node
Macrophage
Th1
Th2
Th17
T reg
T helper cells
Notes: The inflammatory macrophages process some of the tissue debris and place some of that proteinaceous material on its cell wall to present to the lymph nodes. The lymph nodes are where the T cells reside before being sent out on duty. There are proteins on the surface of the macrophages that T cells recognise and in turn T cells develop into their different roles. One of these roles are the T helper cells. They are logistics specialists and help organise the response on the ground by the various inflammatory cells.
It is the balance between these cells that influences the effect. T1 like a nice quick fix and healing process, T2 are the guys who go in and build up fibrous repair (the containment) T17 are trouble, they prolong the inflammatory process (don’t want these guys predominating) T reg cells control the inflammatory response, don’t let it get out of control, dampen it down and keep it orderly

## Slide 24
Th2 cell
Fibroblast
Collagen
Mechanical Stress
Cytokines
Molecular signaling
Myofibroblast
Notes: The recruited fibroblasts continue to produce collagen. Some of them convert to myofibroblasts which help contract the fibrous capsule around the implant and are also involved in the ongoing inflammatory process.

## Slide 25
Evaluation of the effect of SilkSurface® on fibrosis with miniaturized mouse-sized breast implant mimics
Research performed at the Robert Langer Laboratory at MIT, Boston , USA
Smooth Implants
SilkSurface® Implants
Notes: A B6 mouse model has been used to study what happens on the surface of Motiva Implants® when placed in a ‘live situation’ at the Robert Langer Lab, located in the Koch Institute for Integrated Cancer Research Center at MIT.

## Slide 26
Subcutaneous implantation into female mice
Research performed at the Robert Langer Laboratory at MIT, Boston , USA
Notes: Miniature traditional smooth and SmoothSilk®/SilkSurface® surface implants were implanted into female mice behind their mammary glands.

## Slide 27
Gross examination of explanted Mini Control vs. SilkSurface® implant with tissue overgrowth
Traditional Smooth (Control)
SmoothSilk®/SilkSurface®
3 weeks
12 weeks
Research performed at the Robert Langer Laboratory at MIT, Boston , USA
Notes: After 3 weeks some of the implants were removed and the rest removed at 12 weeks. You can see in these pictures the thickened capsules around the traditional smooth implants and the thin filmy capsules around the SmoothSilk®/SilkSurface® implants.

## Slide 28
Low Inflammatory Response Research
SmoothSilk® / SilkSurface® ameliorates fibrosis in B6 mice
Smooth
SmoothSilk® / SilkSurface®
Histological analysis of the tissue capsule surrounding the Smooth and SmoothSilk® / SilkSurface® tiny implants with two different staining techniques.
Research performed at the Robert Langer Laboratory at MIT, Boston , USA
Notes: These are histological slides of the capsules removed. The top row is using H&E stain which looks at the cells and you can see a high cellular infiltration of the smooth implant capsules. The Masson’s Trichome stains the collagen and shows the increased collagen deposition in the capsule around the traditional smooth implant. The dashed red line marks the outside of the capsule.

## Slide 29: Analysis to quantify macrophages in tissue capsules surrounding implants
SilkSurface® decreases fibrosis-dependent innate immune macrophages.
Less macrophages presence with SmoothSilk®/SilkSurface®
Notes: Now want to avoid the fibrotic capsules but also ameliorate the chronic inflammation that we know is at the root of BIA ALCL. Macrophages are key to the chronic inflammatory process that is the foreign body response. They initially attempt to engulph the foreign material but when the material is too large the macrophages multiply and take on different roles. In short they take on a moderator role communicating with and recruiting other immune cells to attack and contain the foreign material. This slide demonstrates the findings of a significant reduction (85%) in the number of macrophages seen on the SmoothSilk®/SilkSurface® implant compared with the traditional smooth implants by 3 weeks and 63% reduction at 6 weeks in the mice study. A reduction in macrophage numbers indicates a dampened down foreign body response to the implant.

## Slide 30
Full-size Human-scale Implants testing in Rabbit Model
Research performed at the Robert Langer Laboratory at MIT, Boston , USA
Notes: Then, at the same lab the study went on to use a rabbit model where full size implants could be used.

## Slide 31
Traditional Smooth (control)
Full-size Human-scale Implants testing in Higher Order Rabbit Model 3-week retrievals
SmoothSilk®/SilkSurface®
Research performed at the Robert Langer Laboratory at MIT, Boston , USA
Notes: Again the findings are the same with thick fibrotic capsules around the traditional smooth implants and thin membranous capsules around the SmoothSilk®/SilkSurface® implants. The rabbit model is used as it more closely resembles what happens in humans.

## Slide 32
Positive outcomes indicated by thin capsules
capsules from re-operations for size change
Post-Market Surveillance – Motiva Implants®
6 months
26 months
5 years
Notes: These photographs are of implants removed for a size change. They demonstrate the typical membranous thin capsule seen in Motiva Implants®

## Slide 33
S. epidermidis biofilm formation (24 h) on different breast implant surfaces
630 x magnification
SmoothSilk®/SilkSurface®
“PU foam imprint” texture
“Salt-loss texture
Traditional Smooth
Independent testing performed by the Center for Biofilm Engineering, Montana State University, USA.
Garth James, PhD1, Laura Boegli, BS.1, John Hancock, BSME2, Brian M. Kinney, MD3. In-vitro Testing of Bacterial Attachment and Biofilm Formation on Different Breast Implant Outer Shell Surfaces 1Montana State University, Bozeman, MT, USA, 2Establishment Labs, Santa Barbara, CA, USA, 3University of Southern California, Beverly Hills, CA, USA. http://meeting.aaps1921.org/abstracts/2018/P8.cgi
PU foam imprint
Notes: These are images of stained bacteria photos taken of biofilm formation on different breast implant surfaces at 24 hours. The Motiva SmoothSilk®/SilkSurface® have significantly less biofilm than the “Salt-loss” textured and “PU foam imprint” breast implant surfaces. Staphylococcus epidermidis is a bacteria that sits on the skin and is harmless on the skin, but is capable of developing biofilm and has been found in breast implant capsules.

## Slide 34
P.aeruginosa biofilm formation (24 h) on different breast implants
SmoothSilk®/SilkSurface®
630 x magnification
“Salt-loss” texture
Traditional Smooth
Independent testing performed by the Center for Biofilm Engineering, Montana State University, USA.
Garth James, PhD1, Laura Boegli, BS.1, John Hancock, BSME2, Brian M. Kinney, MD3. In-vitro Testing of Bacterial Attachment and Biofilm Formation on Different Breast Implant Outer Shell Surfaces 1Montana State University, Bozeman, MT, USA, 2Establishment Labs, Santa Barbara, CA, USA, 3University of Southern California, Beverly Hills, CA, USA. http://meeting.aaps1921.org/abstracts/2018/P8.cgi
“Salt-loss texture
Traditional Smooth
PU foam imprint
Notes: Pseudomonas is a more aggressive gram negative bacteria associated especially with burns infections. It is also capable of developing biofilm. Here again the SmoothSilk®/SilkSurface® has significantly less biofilm after 24 hours growth with this bacteria compared to the macrotextured implants.

## Slide 35
Surface Area & Biofilm
Surface area measured for different breast implants and 24- hour average log(10) CFU/disc (Staphylococcus epidermidis bacteria attachment) to them, based on The Center of Biofilm Engineering Testing at Montana State University.
Loch-Wilkinson, A., Beath, K., Knight, R., Wessels, W., Magnusson, M., Papadopoulos, T., Connell, T., Lofts, J., Locke, M., Hopper, I., Cooter, R., Vickery, K., Joshi, P., Prince, M., Deva, A. Breast implant associated Anaplastic Large Cell Lymphoma in Australia and New Zealand – high surface area textured implants are associated with increased risk. Plastic and Reconstructive Surgery Advance Online Article.
Notes: The texturing process increases the surface area of a breast implant surface. When the different surface areas are plotted against biofilm development we can see there is a close correlation between the surface area and biofilm formation, with the macrotextured surfaces having the most biofilm.

## Slide 36: TrueTissue™ Dynamics: TrueMonobloc® Designed to Improve Mechanical Performance and Facilitate Implant Insertion
ALL COMPONENTS OF THE IMPLANT ARE DESIGNED TO PERFORM AS ONE STRUCTURE
Notes: TrueMonobloc® is a process of linking the components of the implant to create a single structure that is designed for enhanced mechanical performance and ease of implant insertion.

## Slide 37: TrueTissue Technology™: Shell to gel interphase
The chemical structure provides optimal adhesion shell to gel that impact the performance of breast implant. The vinyl at the end of the chains (terminal vinyl) are more reactive than pendant vinyl, increasing the adhesion among the shell and the gel.
Notes: To explain how the gel attaches to the shell we need to look at the chemistry. The ProgressiveGel™ ULTIMA® has more reactive vinyl on the outer ends of the molecules which act as glue attaching to similar vinyl terminals in the shell. This is done in a final curing process in the manufacturing process.

## Slide 38: TrueTissue Technology™: Shell to gel interphase
Optimal adhesion shell to gel by chemical interaction. The presence of vinyl groups in a terminal position favor the shell to gel interphase, producing better adherence shell to gel in the breast implant.
Notes: The terminal vinyl group linkages between shell and gel are shown here. They are strong and do not break apart easily so the shell which has the same elasticity as the gel moves with it.

## Slide 39: Rheology: The Study of the Matter of Flow
Cohesivity
Viscosity
Viscoelasticity
Elasticity
Notes: The gels exhibit rheological properties which determine its functional characteristics: cohesivity, viscosity, elasticity and viscoelasticity

## Slide 40: Cohesivity
Notes: The molecules stick together when stretched out, like people linking hands at full stretch. Bubble gum has high cohesivity as it doesn’t break apart when pulled.

## Slide 41: Viscosity
Notes: Water has a low viscosity and flows easily. But volcanic lava has a higher viscosity and does not flow easily.

## Slide 42: Elasticity
Notes: Elasticity refers to how much an object can be deformed and it restores its original form, for example an spring can return to its original shape.
The opposite is plasticity, play doh or plasticine can`t go back because they are not elastic.

## Slide 43: Viscoelasticity
Notes: Viscoelasticity is a more advanced characteristic that describes a material that is both viscous and elastic when undergoing deformation. Mattresses manufactured with a body moulding foam are viscoelastic. When you get into bed, the mattress undergoes deformation. Your body weight causes the mattress to deform from its original shape. It is how the mattress reacts to this that is critical to how comfortable and supportive it is. Most mattresses, like spring mattresses, are only elastic. No matter how fast or slow you put weight on the mattress, the spring will compresses the same amount. A mattress with an moulding foam is both viscous and elastic under pressure, that is, it reacts both like a spring and like a thick liquid (e.g. molasses). Thus, depending on how you put your weight on the bed, it reacts differently. It means that the bed will shape itself around your body, mirroring itself to your body shape, thus ensuring no uncomfortable pressure points occur. It means when you move, the bed will reshape itself to your new body position. Viscoelasticity equals comfort and support

## Slide 44
Viscoelastic deformation comparison to other gels in the market
Rheological Testing performed at Establishment Labs with the BTC2000 Biomechanical Tissue Characterization Equipment (BTC-2000™). Results Property of Establishment Labs.
Notes: This graph shows the viscoelasticity difference among Motiva Implants® gels and others brands of breast implants, demonstrating that the ProgressiveGel™ ULTIMA® is the most viscoelastic gel in this comparison.

## Slide 45: Motiva Ergonomix® ProgressiveGel™ ULTIMA® for Dynamic Movement
Point of Maximum Projection (PMP) in horizontal and vertical position.
Reference: Booklet: Motiva Doctor. Establishment Labs® 2018.
* The point of maximum projection (PMP) is either at 400 or 450 based upon standing MRI.
Notes: Not only do we have innovations in the surface for increased biocompatibility but also in the implant technology with the gel and shell integrated so become one. They move as one and with the viscoelastic properties in the ergonomix implant act as a Lava lamp becoming round when the patient is flat and moving into an anatomical shape when the patient is upright. A dynamic anatomical implant that is soft.

## Slide 46
2017 progress report at 6 years of a 10 year prospective study with MRI
Safety
No reported rupture, capsular contracture, double capsule or late seromas. No implant replacement due to clinical reasons.
100% of MRI cohort showed no evidence of implant rupture or capsular contracture *MRI cohort 62% of the patients (N=20)
Notes: In a prospective study of 35 cases, 70 Motiva implants have been followed for 6 years. There has been 9.4% replacement due to change in size but no implant replacement for medical reasons; no reported ruptures, no reported capsular contractures, no seromas and no double capsules. 60% of these patients have been followed up with MRI with no detectable problems.

## Slide 47
Notes: This is the paper published in the Aesthetic Surgery Journal September 2017.

## Slide 48
Retrospective Study: 3-year follow-up of 5,813 consecutive causes with Motiva Implants® and competitor experience at Dolan Park Hospital in the United Kingdom performed by 16 Consultant Plastic Surgeons
Complications Rates at 3 years
*Implant ruptures related to contact with metal instruments.
Sforza, MD., Zaccheddu, MD, MSc., Alleruzzo, MD., Seno, MD., Mileto, MD., Paganelli, MD., Sulaiman, MD., Payne, MD., Maurovich-Horvat, PhD Preliminar. 3-year Evaluation of Experience With SilkSurface® and Velvet Surface® Motiva® Silicone Breast Implants: a Single Center Experience with 5813 Consecutive Breast Augmentation Cases. Aesthetic Surgery Journal 2017, 1–12.
Notes: There were no reports of implant rupture due to implant failure. Less than 0.02% of implants had ruptures and these were iatrogenic.

## Slide 49
Retrospective Study: 3-year follow-up of 5,813 consecutive cases with Motiva Implants® and competitor experience at Dolan Park Hospital in the United Kingdom performed by 16 Consultant Plastic Surgeons
Lower Reoperation Rate at 3 years
Notes: A large retrospective study of nearly 6000 consecutive cases followed up at 3 years received Motiva Implants® at the Dolan Park Hospital in the UK. These were performed by a group of 16 consultant plastic surgeons. The group dropped their reoperation rate from 8.43% with another FDA approved implant to less than 1% over the same time period. Of note, this was achieved by the same group of surgeons in the same hospital. The only difference in practice was the change to using Motiva Implants®.

## Slide 50
In the first 7 years since the launch more than 300,000 Motiva Implants® have been placed with only 108 clinically related adverse events reported.
Motiva Implants® Complaint Data Report October 2010 - December 2017.
Complications Rates (N=386,284)
*No cases of implant rupture due to device failure.
Motiva Implants® Post Market Vigilance Report
Notes: Post marketing surveillance of over 300,000 implants have revealed only 108 clinically related adverse events. That is 0.028%.

## Slide 51
Surface & Medical Complications Linkage
Notes: To date we have had traditional smooth surface implants which had a high incidence of capsular contracture, despite lower biofilm contamination. With texturing of implants we have seen reduced capsular contracture but still the development of fibrotic capsules and also seromas and double capsules and even BI-ALCL. They have more biofilm attachment than smooth implants. With the Motiva SmoothSilk®/SilkSurface® we are able to minimize all of these problems.